**easyflex Insulation tube**

**140 x 60 x 13 mm**

**66031400**

Renson Ventilation, IZ 2 Vijverdam, Maalbeekstraat 10, 8790 Waregem – België

Tel. +32 (0)56 62 71 11, fax. +32 (0)56 60 28 51, [info@renson.be](mailto:info@renson.be) www.renson.eu

description

The Easyflex® insulation tube can be used for insulating the flat oval ducts and is therefore ideal for non-insulated areas.

The low thermal conductivity of the foam ensures the correct surface temperature and thus prevents formation of condensation water. The great water vapor diffusion resistance guarantees this feature throughout the life cycle of the installation, resulting in minimal energy loss and higher efficiency.

The insulation tube is also acoustically damping.

product characteristics

* Made of elastomeric foam
* Thermal conductivity: 0,034 W/mK at 0°C (EN ISO 8497)
* Temperature range: -30 to 100°C (EN 14707)

APPLICATION

* The Easyflex ducts that can be insulated with the insulation tube are:
* The flexible Easyflex® duct (G0013110)
* The flat oval duct Easyflex® (G0013126)